Chemical and enzymatic synthetic routes to the diglycidyl ester of 2,5-furandicarboxylic acid

Beatriz Chícharo,a,b Marc Cuesta,c Giacomo Trapasso,b Raul Porcar,d Nuria Martín,c Rocio Villa,e Pedro Lozano,e Sami Fadlallah,a Florent Allais,a Eduardo García-Verdugoc,* and Fabio Aricòb,*

a URD Agro-Biotechnologies Industrielles (ABI), CEBB, AgroParisTech, 3 Rue des Rouges-Terres, 51110 Pomacle, France

b Department of Environmental Sciences, Informatics and Statistics, Ca’ Foscari University of Venice, Via Torino155, 30172 Venezia Mestre, Italy

c Department of Inorganic and Organic Chemistry, University Jaume I, Avda Sos Baynat s/n, E-12071-Castellon, Spain.

d Departamento de Química Orgánica y Bio-orgánica. Facultad de Ciencias. Universidad Nacional de Educación a Distancia (UNED). Avda. Esparta. 28232-Las Rozas. Madrid. Spain.

e Department of Bioquímica y Biología Molecular "B" e Inmunología, Universidad de Murcia, Campus de Espinardo. E-30.100. Murcia, Spain

E-mail: fabio.arico@unive.it, cepeda@uji.es

Abstract

This work focuses on alternative, green synthetic methods for producing a bio-based bis-epoxy compound – namely bis(oxiran-2-ylmethyl) furan-2,5-dicarboxylate (DGF) – in consideration of its potential use as monomer for epoxy resins.  The synthesis of DGF was conducted via transesterification reaction of 2,5-furandicarboxylic acid dimethyl ester (FDME) with glycidol. A variety of homogeneous, heterogeneous, and enzymatic catalysts were investigated, and the syntheses were carried out avoiding any chlorine-based chemicals and employing green media. The homogeneous route yielded the best results when the reaction was conducted in 2-Me-THF as medium and using triethylamine as a catalyst. DGF was isolated as pure in 82% yield through a simple liquid-liquid extraction. In the heterogeneous route, triethylamine immobilized on a polymeric polystyrene-divinylbenzene (PS-DVB) support, led to a lower yield due to a moderate substrate conversion. The chemo-enzymatic route employed Candida antarctica lipase B (CALB) supported on various Supported Ionic Liquid-Like Phases (SILLPs). In this case DGF yield was only of 10-20%. Interestingly, the reaction led to similar results even in the absence of the enzyme, suggesting that the ionic liquid-like phase on the resin was not a passive support, but it actively participated in promoting the transesterification reaction. Thus, the efficiency of several SILLPs as catalysts was evaluated. Among them, the butyl imidazolium chloride SILLP demonstrated superior catalytic performance compared to supported alkyl ammonium salts leading to 79%. Furthermore, its stability resulted very promising, maintaining consistent catalytic efficiency over 12 consecutive cycles.

Keywords: Green chemistry; Renewable Resources; FDCA-based epoxy monomers; Bio-derived Alternatives.

Introduction

The growing interest in using renewable resources to produce polymeric materials is largely driven by environmental concerns and the need for sustainable solutions to the challenges facing the current generation. As a result, the plastic industry is transitioning to more sustainable approaches in developing new products and materials (Bielski and Grynkiewicz, 2021; Zhang and Dumont, 2017). This has led to a rising interest in using natural resources, such as polysaccharides (Zhang et al., 2022; Zhu et al., 2016), lignin (Zhu et al., 2016) and furan based derivatives (Annatelli et al., 2024; Bielski and Grynkiewicz, 2021; Zhang and Dumont, 2017) for the preparation of renewable monomers and synthons, commonly referred as bio-based platform chemicals. A prominent example is related to epoxy resins (ERs), extensively investigated materials with numerous applications in coatings, composites, electronic devices and as thermosets for aerospace industries (Jin et al., 2015; Rahman and Akhtarul Islam, 2022; Rong et al., 2024). Most of the commercially available ERs are produced from diglycidyl ether of bisphenol A (DGEBA), a derivative of fossil-based bisphenol A (BPA) (Scheme 1).

The global epoxy thermosetting polymer production was estimated to be 3 million tons per year, and this value has been growing rapidly since then (Negrell et al., 2017; Yang et al., 2025; Ng et al., 2017), with BPA accounting for more than 90% of the industry's sources for epoxy resins (Giulivo et al., 2016; Ng et al., 2017).

Scheme 1- BPA based epoxy resins synthesis with epichlorohydrin.

The aromatic structure of BPA provides resins with good thermostability and mechanical strength that render them extremely resistant to corrosion (Verma et al., 2020), moisture, and chemicals (Marotta et al., 2018). As a result, these materials are useful for a wide range of applications such as coatings (Verma et al., 2020), composites (Sprenger, 2013), electronic devices (Ho and Wang, 1996; Jin et al., 2015), and thermosets in the Aerospace industry (Guadagno et al., 2014; Rahman and Akhtarul Islam, 2022; Rong et al., 2024). However, BPA is a non-renewable compound that also demonstrated to affect human health being an endocrine-disrupting agent and nephrotoxic compound (Dai et al., 2018). Furthermore, DGEBA is still produced via chlorine-based chemistry employing epichlorohydrin, a well-known carcinogenic, mutagenic, reprotoxic, and endocrine disruptor (Scheme 1). It is also worth noting that epoxy thermosets are very susceptible to hydrolysis, which can increase the risk of human exposure (Ng et al., 2017).

Due to these concerns, many European countries have implemented stricter regulations on BPA-based products (Dai et al., 2018). The scientific community is actively exploring alternative sources for producing epoxy resins that provide similar or superior properties compared to BPA, while improving their safety both on the environment and human health.

Over the years, researchers have explored various natural resources for synthesizing epoxy resins. Among them, vegetable oils (Biermann et al., 2000; Meier et al., 2007) and modified cardanol (Voirin et al., 2014) are the most extensively investigated ones due to their availability, low cost, and desirable characteristics. The resulting epoxy resins prepared using these long aliphatic chains either alone or with aromatic co-monomers, have demonstrated to be promising materials. However, to attain thermal and mechanical properties similar to those of BPA-based materials, the incorporation of aromatic moieties is required (Ng et al., 2017). As a result, new bio-derived monomers started to be investigated. Particularly, in the last few years, furanic-based monomers derived from carbohydrate feedstocks, such as 2,5-bis(hydroxymethyl)furan (BHMF) (Cho et al., 2013), 2,5-furandicarboxylic acid (FDCA) (Deng et al., 2015), and its esters (Marotta et al., 2018), 5,5'-(oxy-bis(methylene)bis-2-furfural (OBMF) (Meng et al., 2019b), and propane-2,2-diylbis(furan-5,2-diyl))dimethanol (bFdE) (Cho et al., 2013) showed to be promising candidates in this field (Figure 1).

Figure 1- Furanic-based epoxy monomers already reported in the literature.

Data collected demonstrated that incorporating a furan rings into the polymer structure improves the thermal properties of the resin compared to traditional petroleum-based counterparts (Meng et al., 2019b). Epoxy FDCA-based resins displayed higher glass transition temperature (Tg) values compared to other bio-based epoxy resins (Meng et al., 2019a). This observation was ascribed to the formation of hydrogen bonds between the oxygen in the furan ring and the alcohols formed during the curing of the epoxide, providing the resin superior stability which eventually reflects on their thermal properties (Liu et al., 2020).

Although resins based on epoxy FDCA monomers displayed great promise due to their enhanced thermal properties and renewable origin, the synthetic routes for producing the key epoxide intermediates are far from being environmentally friendly.

In this context, the synthesis of the diglycidyl ester of 2,5-furandicarboxylic acid (DGF), also known as bis(oxiran-2-ylmethyl) furan-2,5-dicarboxylate, serves as a case study.

Currently, there are two main methods for synthesizing DGF, both of which present significant environmental challenges. The first method involves the use of chlorinated compounds. Examples include: (i) the reaction of epichlorohydrin (ECH) with FDCA (Marotta et al., 2018); or (ii) the reaction of 2,5-furandicarbonyl dichloride with glycidol (Liu et al., 2020) (Scheme 2, reaction (I)). The second method follows a two-step process in which the furan monomer is initially reacted with an allylic compound, such as allyl bromide (Deng et al., 2015; Meng et al., 2019a) or allyl alcohol (Nameer et al., 2018), to form allylic ester derivatives, which are then oxidized to the respective epoxide using strong oxidizing agents like m-chloroperoxybenzoic acid (m-CPBA) (Deng et al., 2015; Meng et al., 2019a; Nameer et al., 2018) (Scheme 2, reaction (II)).

Scheme 2- Examples of FDCA-based epoxy monomers synthesis, with a renewable source and non-green synthesis ((I), (II)) and our approach (III).

In the pursuit of alternative halide-free methods, the transesterification of the FDCA ester, furan-2,5-dicarboxylate (FDME), with glycidol was also reported using potassium cyanate (KOCN) as a catalyst (Marotta et al., 2018). However, this approach relies on a highly toxic catalyst and lacks detailed procedural descriptions. Considering these challenges, the present work investigates alternative and greener synthetic approaches to DGF, starting from FDME utilizing homogeneous, heterogeneous, and enzymatic promoters and catalysts without relying on chlorine chemistry (Scheme 2, reaction (III)) and adopting green media whenever possible.

Experimental

General information

All reagents and solvents were purchased from Sigma-Merck and employed without any further purification. Reactions were conducted in a Drysyn at the required temperature, measured with a thermocouple. Reactions were monitored by TLC on an aluminum strip coated with silica gel 60 F254 from Merck, revealed under UV light (254 nm) and in the presence of permanganate staining solution. 1H NMR spectra of all monomers were conducted through a spectrometer Bruker 400 MHz in CDCl3. 13C NMR spectra were recorded on Brucker Fourier 400 (101 MHz) in CDCl3. FTIR spectra were acquired with a MIRacle single reflection ATR diamond/ZnSe accessory in a JASCO FT/IR-6200 instrument. Elemental analysis data were acquired with a TruSpec Micro CHNS & O Elemental Analyzer (LECO).

Synthesis of diglycidyl ester of 2,5-furandicarboxylic acid (DGF) via homogenous catalysis

In a typical reaction 0.5 g (2.71 mmol) of FDME was reacted with 4.0 mol eq. of glycidol in the presence of 0.1 mol eq. of catalyst in 10 mL of 2-methyltetrahydrofuran (2-MeTHF) at 60 °C in a two neck round bottom flask with a water condenser. To drive the equilibrium reaction towards the product formation, N2 flow was used, which aided the methanol removal. The reaction was monitored by 1H NMR. Upon completion, the solvent, if any, was evaporated and the product was isolated through a liquid-liquid extraction with ethyl acetate and water. The pure compound was obtained as a white solid with 82% isolated yield. The product can be further purified by recrystallization in hot methanol (final yield of 64%).

1H NMR (400 MHz, CDCl3) δ 7.27 (d, J = 0.8 Hz, 1H1), 4.65 (dd, J = 12.2, 3.2 Hz, 1H4), 4.20 (dd, J = 12.2, 6.2 Hz, 1H4), 3.37 – 3.30 (m, 1H5), 2.90 (td, J = 4.5, 4.0, 0.8 Hz, 1H6), 2.73 (ddd, J = 4.9, 2.6, 0.8 Hz, 1H6); 13C NMR (101 MHz, CDCl3) δ 157.6 (C3), 146.5 (C2), 119.0 (C1), 66.0 (C4), 49.1 (C5), 44.8 (C6).

ATR-FT-IR: 3108, 1710, 1586, 1575, 1521, 1517, 1457, 1448, 1343, 1268, 1133, 1036, 989, 982, 941, 904, 866, 851, 815, 765, 754 cm-1.

MS: [M+Na]+ =  Calc. for C12H12NaO7 291.0475; Found 291.0481.

Melting Point: 89.97 ºC

Preparation and characterization of supported heterogenous catalysts S-Et3N and S-NMPy

Synthesis of S-Et3N: 1.0 g of Merrifield resin (macroporous resin, 5.5 meq/g, 5.5 mmol) was suspended in 10 mL of N,N-dimethylformamide (DMF) in a reaction vessel. Subsequently, 4.0 mL of diethylamine (38.69 mmol) were added to the suspension. The reaction mixture was stirred at 75 °C for 24 hours to ensure thorough functionalization. After reaction completion, the polymer was isolated by vacuum filtration and washed with methanol (3 × 20 mL) to remove residual reagents and byproducts. The resulting functionalized polymer was dried in a vacuum oven at 50 °C until a constant weight was achieved.

ATR-FT-IR: 2966, 2927, 2797, 1508, 1448, 1382, 1369, 1288, 1199, 1165, 1058, 1019, 843, 823, 809, 771 cm-1.

Elemental analysis, experimental: %N 6.73; Loading of compound S-Et3N: 4.78 meq/g.

Synthesis of S-NMPy: 1.0 g of Merrifield resin (macroporous resin, 5.5 meq/g, 5.5 mmol) was suspended in 10 mL of DMF in a reaction vessel. Subsequently, 1.36 mL of pyrrolidine (16.5 mmol) were added to the suspension. The reaction mixture was stirred at 75 °C for 24 hours to promote functionalization. After reaction completion, the polymer was isolated by vacuum filtration and thoroughly washed with methanol (3 × 20 mL) to remove residual reagents and byproducts. The resulting functionalized polymer was dried in a vacuum oven at 50 °C until a constant weight was achieved.

ATR-FT-IR: 2962, 2924, 2873, 2777, 2729, 1509, 1445, 1421, 1374, 1347, 1347, 1324, 1290, 1252, 1252, 1199, 1125, 1019, 879, 841, 820, 627, 616 cm-1.

Elemental analysis, experimental: %N 7.176; Loading of compound S-NMPy: 4.99 meq/g.

Synthesis of DGF via supported heterogenous catalysts S-Et3N and S-NMPy

In a typical reaction, 100 mg of dry catalyst (S-Et3N or S-NMPy) and 50 mg of activated molecular sieves (4 Å) were suspended in a solution of 100 mg of FDME (0.54 mmol) dissolved in 1.0 mL of 2-MeTHF. The reaction mixture was stirred at 60 °C, and 88 µL of glycidol (1.32 mmol) were added dropwise. The mixture was then heated at 60 °C for 6 hours. After cooling to room temperature, the reaction crude was filtered to remove the catalyst and molecular sieves. The solvent was subsequently removed under reduced pressure. The resulting white solid was dried under vacuum to constant weight for further characterization.

Preparation and characterization of supported ionic liquids (SILLPs)

SILLP-1 (BuIMCl): 5.0 g of Merrifield resin (macroporous resin, 5.5 meq/g, 27.5 mmol) was suspended in 75 mL of DMF in a reaction flask. To this suspension, 12 mL of 1-butylimidazole (91 mmol) were added. The reaction mixture was stirred at 50 °C for 24 hours to facilitate functionalization. After reaction completion, the polymer was recovered by vacuum filtration and washed thoroughly with methanol (3 × 20 mL) to remove unreacted reagents and byproducts. The functionalized polymer was dried in a vacuum oven at 50 °C until constant weight was achieved.

ATR-FT-IR: 3132, 3054, 2959, 2929, 2871, 1637, 1558, 1456, 1424, 1361, 1328, 1155, 851, 816, 751 cm-1.

Elemental analysis, experimental: %N 8.75; Loading of compound SILLP-1: 3.12 meq/g.

SILLP-2 (BuIMNO3): 250 mg of SILLP-1 (macroporous resin, 5.5 meq/g, 1.375 mmol) were suspended in 27.5 mL of 1 M NaOH and stirred at room temperature for 24 hours. The polymer was then washed with water (3 × 10 mL) and suspended in 7 mL of 1 M HNO3, followed by stirring at room temperature for another 24 hours. The polymer was filtered under vacuum, washed with water (3 × 10 mL), and dried in a vacuum oven at 50 °C until constant weight.

ATR-FT-IR: 3146, 3103, 2963, 2932, 2874, 1636, 1561, 1454, 1331, 1155, 827, 749 cm-1.

Elemental analysis, experimental: %N 12.72; Loading of compound SILLP-2: 3.03 meq/g.

SILLP-3 (TributylamineCl): 2.0 g of Merrifield resin (macroporous resin, 5.5 meq/g, 11 mmol) was suspended in 10 mL of acetonitrile. Then, 3.27 mL of tributylamine (13.7 mmol) were added to the mixture. The reaction was stirred at 60 °C for 24 hours. After the reaction, the polymer was recovered by vacuum filtration and washed thoroughly with methanol (3 × 20 mL). The final product was dried in a vacuum oven at 50 °C until constant weight.

ATR-FT-IR: 2960, 2926, 2869, 1731, 1622, 1512, 1464, 1376, 1170, 1060, 860, 860, 860, 860, 860, 817, 735 cm-1.

Elemental analysis, experimental: %N 3.63; Loading of compound SILLP-3: 2.59 meq/g.

SILLP-4 (TributylamineNO3): 250 mg of SILLP-3 (macroporous resin, 5.5 meq/g, 1.37 mmol) were suspended in 27.5 mL of 1 M NaOH and stirred at room temperature for 24 hours. The polymer was then washed with water (3 × 10 mL) and resuspended in 7 mL of 1 M HNO3, followed by stirring at room temperature for another 24 hours. The treated polymer was filtered under vacuum, washed with water (3 × 10 mL), and dried in a vacuum oven at 50 °C until constant weight.

ATR-FT-IR: 2962, 2931, 2874, 1623, 1457, 1326, 1142, 1115, 1037, 863, 828, 736 cm-1.

Elemental analysis, experimental: %N 6.68; Loading of compound SILLP-4: 2.39 meq/g.

SILLP-5 (IM-SO3-Sc(OTf2)): The synthesis and characterization of SILLP-5 was performed as reported in previous literature [Peris et al. 2019].

SILLP-6 (IM-SO3H): The synthesis and characterization of SILLP-6 was performed as reported in previous literature [Peris et al. 2019].

Preparation and characterization of enzymes with supported ionic liquids (SILLPs)

General procedure for the synthesis of SILLPs: A Merrifield resin (2.0 g, mocroporous or gel type) was suspended in 25 mL of the corresponding imidazole. The system was heated at 80 ºC. After 24 h, the polymer was filtered, washed with DMF (3 × 20 mL), MeOH (3 × 20 mL), CH2Cl2 (3 × 20 mL) and dried under vacuum at 50 ºC (Burguete et al., 2011).

Lipase immobilisation on to SILLPs was performed as reported in previous literature [Lozano et al. 2012] (I. R1= H-, R2= CH3- (3.10 mg CALB / g) microporous; II. R1= H-, R2= CH3(CH2)3- (4.81 mg CALB / g); III. R1= CH3-, R2= CH3(CH2)9- (3.32 mg CALB / g); IV. R1= H-, R2= CH3- (3.32 mg CALB / g); V.  R1= H-, R2= CH3(CH2)3- (3.10 mg CALB / g); VI. R1= CH3-, R2= CH3(CH2)9- (3.69 mg CALB / g)).

Synthesis of DGF catalyzed by immobilized catalyst based on SILLPs

100 mg of dry catalyst and 50 mg of activated molecular sieves (4Å) were suspended in a solution of 100 mg of FDME (0.54 mmol) in 1.0 mL of 2-MeTHF. The mixture was stirred at 60 ºC and 88 µL of glycidol (1.32 mmol) were added. Then, the mixture was heated for 6 hours Finally, the mixture reaction was filtered and the solvent was removed under reduced pressure. The product obtained was dried in a vacuum pump.

Results & discussion

DGF synthesis via homogenous catalysis

The synthesis of the diglycidyl ester of 2,5-furandicarboxylic acid (DGF) was firstly investigated employing a homogenous catalysis. In a typical reaction FDME, synthesized according to previously reported procedures (Trapasso et al., 2023, 2022), was reacted with an excess of glycidol (4.0 mol eq.) in the presence of a base (10% mol) at 60 °C (Table 1) for 2 hours. To drive the reaction equilibrium toward the desired product, an N₂ flow was employed to facilitate the removal of methanol forming as by-product of the transesterification.

It is important to note that glycidol can easily undergo homo-polymerization even at room temperature, which results in the formation of highly branched polymers (Sandler and Berg, 1966; Trzebicka et al., 2024). This tendency underscores the necessity of adding a solvent to the reaction mixture. In this case, we chose to use 2-MeTHF, since it is considered a green solvent.

Table 1- Catalyst screening for the synthesis of DGFDC.

| # | Catalyst | t (h) | T (°C) | Conv. (%) | Selectivity (%)a |  | DGF Yield (%)a |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | DGF | MGF |  |
| 1 | Et₃N | 2 | 60 | 72 | 30 | 70 | 22 |
| 2 | Et₃N | 5 | 60 | 100 | 100 | 0 | 100 |
| 3 | DABCO | 2 | 60 | 61 | 23 | 77 | 14 |
| 4 | NMPy | 2 | 60 | 74 | 30 | 70 | 22 |
| 5 | NMPy | 7 | 60 | 100 | 85 | 15 | 85 |
| 6 | TBD | 2 | 60 | 62 | 23 | 77 | 14 |
| 7 | DBU | 2 | 60 | 28 | 10 | 90 | 3 |
| 8 | DMAP | 2 | 60 | 64 | 22 | 78 | 14 |

Reaction conditions: 2.71 mmol of FDME (0.5 g), 4.0 molar equivalents of glycidol and 10 mol% of base, in 10 mL of 2-MeTHF. a Calculation via 1H NMR spectroscopy.

Several homogeneous nitrogen-containing bases were tested for this transesterification including triethylamine (Et3N), N-methyl pyrrolidine (NMPy), 1,5,7-triazabicyclo[4.4.0]dec-5-ene (TBD), 1,8-diazabicyclo(5.4.0)undec-7-ene (DBU), 1,4-diazabicyclo[2.2.2]octane (DABCO), 4-dimethylaminopyridine (DMAP). Data collected showed discrete to good substrate conversion ranging from 28 to 74%. Among them, the most promising results were achieved with Et3N (#1; Table 1) and NMPy (#4; Table 1) as they both yielded DGF in 22% yield after a two-hour reaction. When these bases were tested for a longer reaction time (#2 and #5; Table 1), a complete conversion of FDME was observed. Nevertheless, the synthesis performed in the presence of Et3N proved to be more efficient leading to DGF in quantitative yield after 5 h. Thus, further optimizations were conducted only using triethylamine as base (Table 2).

Table 2- Optimization of the reaction condition for DGF synthesis using Et3N as a base.

| # | Et3N (% mol) | Conc (mM) | Glycidol (mol eq.) | Conv. (%) | Selectivity (%) |  | DGF Yield (%) |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | DGF | MGF |  |
| 1 | 10 | 0.27 | 4.0 | 100 | 100 | - | 100 (82)a |
| 2 | 5 | 0.27 | 4.0 | 95 | 62 | 38 | 59 |
| 3 | 10 | 0.27 | 3.0 | 95 | 65 | 35 | 62 |
| 4 | 10 | 0.54 | 4.0 | 100 | 92 | 8 | 92 |
| 5 | 10 | 0.81 | 4.0 | 98 | 78 | 22 | 76 |
| 6 | 10 | Neat | 4.0 | 96 | 76 | 24 | 73 |

Reaction conditions: 2.71 mmol of FDME with glycidol and triethylamine in 2-MeTHF at 60 °C for 5 hours. Conversion, selectivity and yields were evaluated via proton NMR; a Isolated yield.

A trial was then carried out decreasing the quantity of the base from 10% mol to 5% mol. NMR data collected from the reaction mixture indicated an incomplete FDME conversion and lower selectivity toward the desired product (#1-2; Table 2). An experiment was conducted diminishing the quantity of glycidol to 3.0 mol eq, however this led to a reduction of both conversion and selectivity (#1 and #3; Table 2).

Few trails were also conducted at higher substrates concentration (#4-6; Table 2); however, diminishing the amount of solvent led to reduced conversion and selectivity to the desired product most probably due to the concurrent glycidol self-polymerization.

It should be also mentioned that FDME transesterification, being a thermodynamically driven reaction, is favored by methanol removal from the reaction mixture. To this end, all the above reported trials were conducted at 60 °C. Nevertheless, the evaporation of 2-Me THF was always observed despite its higher boiling point (78 °C). This seems to suggest the formation of an azeotropic mixture 2-MeTHF:MeOH that propels the reaction favoring DGF formation. It is well documented in the literature the azeotropic mixture methanol:THF (Li et al., 2013), therefore, a similar behavior may also occur when using 2-MeTHF, due to the similarities between the two tetrahydrofuran-based solvents.

Different media were also employed under the optimized conditions reported in #1 Table 2 (Figure 2, Table SI. 1, Supporting Information - SI). The outcomes demonstrated similar results for the reactions carried out in acetonitrile and CPME, showing significantly lower conversion and selectivity values as opposed to 2-MeTHF. This suggests that the solvent truly exerts a crucial role in the reaction and its co-evaporation with methanol facilitates the transesterification reaction.

Figure 2- Solvent testing (Table S1, SI); Conversion and selectivity were evaluated via proton NMR. (Table SI. 1. SI).

Gram-scale trials were also attempted testing the reaction on 1.0 g and 5.0 g of FDME. These tests were performed in the optimal conditions previously found (#1, Table 2) with the addition of a Dean Stark apparatus and N2 flow to facilitate methanol removal. However, these experiments led to lower selectivity (53-67%) and moderate yields (46-57%) when compared to the 0.5 gram scale previously employed (Table SI. 2, SI). In the case of large-scale reactions, it was observed a less prominent solvent (MeOH) evaporation compared to the smaller scale trials, even when maintaining the previously determined optimal concentration. As this is a thermodynamically driven reaction, there may have been some changes in the reaction equilibrium that hindered the efficiency of the gram scale reactions.

DGF synthesis via heterogenous catalysis

Using molecular catalysts on solid materials has been an effective strategy to intensify catalytic processes while retaining the advantages of homogeneous catalysts. Considering the results obtained with the homogeneous bases, two different supported bases, analogous to triethylamine (S-Et3N) and methylpyrrolidine (S-NMPy), were evaluated for the transesterification reaction. Their immobilization on polymeric polystyrene-divinylbenzene (PS-DVB) resins offers a convenient method for product recovery and enables the catalyst to be reused across multiple cycles.

Figure 3- Supported heterogenous catalyst from triethylamine (S-Et3N) and methylpyrrolidine (S-NMPy).

Unfortunately, the results from the supported catalysts were disappointing compared to their performance in the homogeneous system. In fact, both S-Et3N and S-NMPy showed significantly lower activity when employed under similar reaction conditions used for the related bases (Tables 1-2). Namely, in the presence of S-Et3N when using 2.4 mol eq. of glycidol relative to FDME 0.27 M in 2-MeTHF at 60 °C for 5 hours, the yield reached only 18% for DGF (#1, Table 3). Increasing the glycidol/FDME ratio led to slight improvements, with DGF yields reaching 27% (#2, Table 3). Besides, when the transesterification was conducted using the supported pyrrolidine derivative, the yield was only 4% with an almost total selectivity towards MGF (#3, Table 3).

Table 3- DGF employing supported bases

| # | Cat. (% mol) | Conc (M) | Glycidol (mol eq.) | Conv. (%) | Selectivity (%) |  | DGF Yield (%) |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | DGF | MGF |  |
| 1 | S-Et3N (10) | 0.27 | 2.4 | 51 | 35 | 65 | 18 |
| 2 | S-Et3N (10) | 0.27 | 4.9 | 63 | 43 | 57 | 27 |
| 3 | S-NMPy (10) | 0.27 | 2.4 | 38 | 10 | 89 | 4 |

Reaction conditions: FDME (0.27 M) with glycidol and triethylamine in 2-MeTHF at 60 °C for 5 hours. Conversion, selectivity and yields were evaluated via proton NMR.

The poor performance of these supported catalysts, in terms of activity and selectivity, can be ascribed to the slower reaction rate compared to homogeneous conditions. The immobilization of the catalyst most likely limited the access of the reactants to the active sites, making the reaction less efficient. Moreover, the use of the supported system seemed to promote the self-polymerization of glycidol, which further lowered the yield of the desired product.

DGF synthesis via chemo-enzymatic catalysis

The potential of enzymes as a green alternative for the transesterification reaction was also explored. Enzymes represent a versatile and highly efficient class of catalysts for achieving selective, clean, and sustainable chemical transformations, particularly in non-aqueous environments. Among them, lipases are the most extensively utilized biocatalysts in green media, such as ionic liquids (ILs), supercritical fluids, and deep eutectic solvents (DES) with low water content (Lozano et al., 2015). In this view, lipases could provide an eco-friendly route for the transesterification of FDME with glycidol to produce DGF.

The development of materials based on ILs, where IL-like moieties are covalently attached to solid supports (Supported Ionic Liquid-Like Phases, SILLPs), provides a valuable tool for creating IL-based microenvironments (Migowski et al., 2023). Such materials serve as “self-organized solid ionic solvents,” exhibiting properties similar to their bulk IL counterparts, making them suitable for continuous biocatalytic processes and as supported catalytic IL-phases.(Villa et al., 2019) Additionally, SILLPs can enhance catalyst performances by aiding enzyme activation, improving activity and stability, and influencing selectivity. These supported systems combine the advantages of biocatalysis in ionic liquid media with the enhanced stability and reusability provided by the immobilized enzyme (Migowski et al., 2023). Building on this (Lozano et al., 2012; Migowski et al., 2023; Villa et al., 2021), several SILLPs bearing different alkyl imidazolium moieties were evaluated, based on gel-type or microporous polymeric polystyrene-divinylbenzene (PS-DVB) resins as support for the immobilization of Candida antarctica lipase B (CALB). These immobilized enzymatic catalysts were tested for the transesterification of FDME with glycidol (Figure 4).

Figure 4 - Evaluation of different CALB-SILLPs (100 mg) 0.54 M of FDME in 2-Me-THF and 2.4 equivalents of glycidol 60 oC, 6 hours (Table SI.3) (blue: MGF; red: DGF).

Figure 4 compares the catalytic performance of CALB immobilized on different SILLPs. Each support was modified with imidazolium groups containing various alkyl substituents (methyl, butyl, and 2-methyl-decyl). Furthermore, the commercially available Novozym 345 was also evaluated. The results indicate that all biocatalysts, regardless of the type of support, led to conversion of FDME from 56-72% with a preference towards MGF. The yield for the desired DGF ranged between 10-20%, while the MGF exhibited higher yields of ca 50%. The best catalytic performance was observed with the CALB immobilized onto macroporous support bearing a butyl substituent, achieving approximately 20% yield for the di-substituted ester. This suggests that macroporous resin slightly enhances catalytic efficiency compared to microporous supports. The improved performance of macroporous systems is likely due to their enhanced accessibility to reactive sites (Sherrington, 1998). The presence of permanent porosity in absence of swelling allows for more effective enzyme-substrate interactions, which in turn increases overall catalytic activity. In contrast, for gel-type resins, diffusion of reagents is limited to those systems where the resins are fully swell in the presence of a solvent and may become a limiting factor. This diffusion limitation can slightly reduce the catalytic activity of these systems, as the substrates may not reach the active sites as easily or uniformly as in the microporous type resins. It should be noted that the Novozym 435 provided very similar results to those obtained with our systems, even though its enzyme loading is significantly higher. This suggests that the efficiency of our supported systems is comparable in terms of catalytic activity, despite using a lower lipase loading.

Unexpectedly, when the reaction profile was monitored and compared using the SILLP in the absence of CALB, similar conversion rates of FDME and yields of mono- and di-substituted esters were observed with the macroporous resin containing butyl substitution (Figure SI.1, SI). The fact that the reaction proceeded similarly without the enzyme suggests that the ionic liquid-like phase on the resin is not just a passive support, but it actively participates in the catalysis. This could be ascribed to the ionic liquid moieties on the SILLP having weak acidic or basic properties, which might facilitate the nucleophilic attack of glycidol on FDME, even without the enzyme. Additionally, the ionic liquid-like phase might create a microenvironment that enhances the transesterification reaction. This microenvironment could stabilize the transition states during the reaction, further promoting its efficiency. The influence of solvent effects caused by ionic liquids, which is well-known in the literature, likely plays a role in this catalytic activity (Hsieh et al., 2023; Schindl et al., 2020). In fact, simple quaternary alkyl ammonium salts showed to promote the transesterification of methyl esters with glycidol, leading to the formation of glycidyl esters (Tanaka et al., 2022, 2019). The proposed mechanism involves the activation of glycidol by the quaternary alkyl ammonium chloride, where chloride anions attack the epoxide, generating an active anionic species that drives the reaction forward.(Hatano et al., 2018)

Considering these observations, the catalytic behavior of the butyl SILLPs (SILLP-1 and SILLP-2) was compared to the one of supported alkyl ammonium salts derived from tributylamine, using Cl⁻ (SILLP-3) and NO₃⁻ (SILLP-4) as counterions, and the catalytic activity was evaluated after one hour (Figure 5). The imidazolium-based systems showed higher conversion rates (39% vs. 28%) and yields towards DGF. Specifically, the imidazolium system yielded 5% DGF and 39% MGF, whereas the alkyl ammonium system produced only 3% DGF and 25% MGF.

When NO₃⁻ was used as the counterion, a sharp decline in activity was observed, with conversions dropping below 1%. This is likely because Cl⁻ is a stronger nucleophile than NO₃⁻. Cl⁻, being smaller and having a concentrated charge, is more reactive and effective in nucleophilic substitution reactions. This highlights the critical role that the choice of counterion plays in determining the efficiency of these catalytic systems.

The superior performance of the imidazolium system is likely attributed to the presence of additional hydrogen atoms in the imidazolium ring (Weber et al., 2013). These hydrogens can form extra hydrogen bonds, which may enhance catalytic activity by stabilizing intermediates during the reaction. This interaction can lead to more efficient and selective catalysis compared to alkyl ammonium salts.

Figure 5 - A) catalytic behavior of the butyl SILLPs compared to the one of supported alkyl ammonium salts (blue: MGF; red: DGF); B) Comparison of the spectra obtained to highlight the formation of side products.

Additionally, it is important to note that alkyl ammonium salts tend to promote the self-polymerization of glycidol leading to a less selective process as illustrated in Figure 5B. This highlights the advantage of imidazolium-based systems in preventing side reactions and maintaining higher selectivity for the targeted product.

To further investigate the effect of SILLP structures, catalysts based on supported ionic liquids incorporating different Brønsted and Lewis acid sites were evaluated. The catalyst containing scandium triflate (Sc(OTf)₃) as a Lewis acid demonstrated a slight improvement in performance, with 8% yield of DGF and 41% yield of the MGF monomer. In contrast, the incorporation of sulfonic acid groups (-SO₃H) as Brønsted acid sites resulted in a significant reduction in catalytic efficiency, with lower yields of the target esters. This suggests that Lewis acid sites, such as Sc³⁺, enhance catalytic activity by coordinating with the carbonyl group of the ester, facilitating nucleophilic attack. On the other hand, strong Brønsted acids may interfere with the reaction environment, promoting side reactions or creating less favorable conditions for ester formation.

The modest improvements in conversion and yield obtained for the system bearing scandium are outweighed by the added complexity and cost of synthesizing this system, using rare and expensive metals. From an industrial perspective, the application of SILLPs without the need for such intricate modifications would be far more advantageous in terms of cost and efficiency. The butyl imidazolium chloride SILLP, which demonstrated promising performances, offers a simpler, more scalable, and cost-effective solution, making it better suited for large-scale processes. The use of readily available materials, along with the avoidance of expensive metals and complex synthesis routes, positions the systems as a more viable option for further optimization.

A key aspect of working with immobilized catalysts is ensuring their stability to develop systems suitable for practical applications. To emphasize this, the experiment was conducted at 60 °C for 6 hours in 2-MeTHF in the presence of the SILLP-1 catalyst. Although these are not optimal conditions, this study allowed for a clear assessment of the catalyst's inherent stability and reusability, independent of maximum efficiency conditions. After each cycle, the supported catalyst was filtered and reused in subsequent reactions. The results (Figure SI.2, SI) demonstrated that the catalyst maintained stable performance over 12 consecutive cycles without significant loss in catalytic efficiency, confirming its robustness and reusability. The slight fluctuations observed can likely be attributed to the fact that the solid catalytic phase was not thoroughly washed between cycles, potentially leading to minor residue buildup or activity variation. Nonetheless, the overall stability of the system demonstrates its suitability for repeated use, enhancing its practical value.

Having established the stability of the catalyst, subsequent efforts were focused on optimizing the reaction conditions to enhance the conversion of FDME and improve selectivity toward the diester, aiming for greater efficiency in the catalytic process.  Firstly, the effect of an increased glycidol amount was evaluated. As the excess of glycidol was raised from 2.4 to 4.0 mol eq. (#1 vs #2, Table 4) the conversion slightly increased together with DFG yield. As the reaction time was increased from 6 to 12 hours, no significant improvement in DFG yield was detected (#3, Table 4). Further increase of glycidol excess induced an increase in the yield to 43% of DGF (#4, Table 4).

Table 4- Optimization of the reaction condition for DGF synthesis using SILLP-1 as immobilized catalyst

| # | Time (h) | Temp. (oC) | Solvent | Glycidol (mol eq.) | Conv. (%) | Selectivity (%) |  | DGF Yield (%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | DGF | MGF |  |
| 1 | 6 | 60 | 2-MeTHF | 2.4 | 75 | 26 | 73 | 20 |
| 2 | 6 | 60 | 2-MeTHF | 4 | 85 | 35 | 65 | 29 |
| 3 | 12 | 60 | 2-MeTHF | 4 | 85 | 38 | 62 | 33 |
| 4 | 12 | 60 | 2-MeTHF | 6 | 93 | 46 | 54 | 43 |
| 5 | 24 | 60 | 2-MeTHF | 2.4 | 84 | 38 | 62 | 32 |
| 6 | 24 | 90 | 2-MeTHF | 2.4 | 91 | 56 | 44 | 51 |
| 7 | 24 | 90 | CPME | 2.4 | 68 | 23 | 77 | 16 |
| 8 | 12 | 90 | ACN | 2.4 | 94 | 60 | 40 | 56 |
| 9 | 24 | 90 | ACN | 2.4 | 98 | 81 | 19 | 79 |

Reaction conditions: FDME (0.54 M) in 2-MeTHF 125 mg supported catalyst; Conversion, selectivity and yields were evaluated via proton NMR.

Given that the increase in DGF performance did not result in a high level of yield, and the use of a large excess of glycidol is problematic due to the need to separate the excess at the end of the reaction, we shifted our focus to experiments evaluating the effect of temperature using only 2.4 equivalents of glycidol. The reaction was performed at 60 °C and under reflux at 90 °C (#5-6, Table 4). The results demonstrated that under reflux, high conversion and a yield of up to 51% could be achieved. Finally, the effect of the solvent was evaluated (#6-7 and 9, Table 4). When acetonitrile (ACN) and CPME were tested as solvents, ACN demonstrated the highest yield, achieving 79% of DGF. By reducing the reaction time to 12 hours in ACN, a yield comparable to that obtained in 2-MeTHF over 24 hours was achieved (#6 vs. #8 and #9, Table 4). These results clearly highlight the significant influence of the solvent on the reaction when SILLP-1 is used as a catalyst. A balance must be established between the reaction's efficiency and the environmental impact of the solvent to optimize the process. It should also be noted that the effect of the media depends on the type of catalyst - homogeneous or heterogeneous - and the related catalytic cycle involved. This is evident in the different results collected in the transesterification when using Et3N and SILLP-1 as promoters using ACN or Me-THF as reaction media.

Conclusions

In this study, we investigated alternative, eco-friendly synthetic methods for FDCA-based bis-epoxy monomers starting from FDME, utilizing homogeneous, heterogeneous, and enzymatic catalysts without relying on chlorine chemistry.

The homogeneous method led to the best results, achieving 82% isolated yield of DGF from a milligram-scale reaction. This was accomplished with minimal purification after a straightforward transesterification reaction conducted at 60 °C, using Et3N as a catalyst. Interestingly, the solvent used during the reaction, 2-Me-THF, seemed to form an azeotropic mixture with methanol, which helped drive the reaction forward. However, for gram-scale reactions, reaction yield decreased, being just moderate. Since this is a thermodynamically driven reaction, there may have been changes beyond our understanding that have affected its efficiency.

The results for the homogeneous route were then used to develop a heterogeneous catalyst made by immobilizing triethylamine and methylpyrrolidine on a polymeric polystyrene-divinylbenzene (PS-DVB) support (S-Et3N and S-NMPy, respectively). However, their activity was significantly reduced compared to the homogeneous process, with conversions of only 63% for S-Et3N and 38% for S-NMPy.

Chemo-enzymatic route was then explored. Candida antarctica lipase B (CALB) was supported on several SILLPs based on gel-type or microporous polymeric polystyrene-divinylbenzene (PS-DVB) and bearing different alkyl imidazolium moieties. All biocatalysts tested, regardless of the type of support, produced FDME conversions from 56 to 72%, with a preference for the mono-substituted ester. The best catalytic performance was observed with CALB immobilized onto gel-type support bearing a butyl substituent. Interestingly, the reaction proceeded similarly without the supported enzyme suggesting that the ionic liquid-like phase on the resin is not just a passive support but actively participates in the catalysis.

The catalytic performance of butyl imidazolium chloride SILLP was found to be superior to that of supported alkyl ammonium salts and catalysts incorporating different Brønsted and Lewis acid sites within the supported ionic liquids in the production of DGF, showing higher conversion rates and yields. The stability of butyl imidazolium chloride SILLP was also promising, maintaining consistent catalytic efficiency over 12 consecutive cycles. Efforts to optimize reaction conditions led to the identification of ACN as the solvent with the highest yield, achieving 79% of DGF.

In conclusion, we have developed two viables high yielding synthetic approaches to DGF employing either a homogenous (Et3N) or heterogeneous (SILLP-1) catalyst. This case study underscores the need for further advancements in the development of renewable epoxy monomers through greener catalytic methods, whether homogeneous, heterogeneous, or using biocatalytic methods.

Author contributions

Conceptualization, supervision and Writing – review & editing: E. García-Verdugo, F. Aricò; Funding acquisition: E. García-Verdugo, F. Aricò, P. Lozano, N. Martín. Supervision and Writing – review & editing: S. Fadlallah, F. Allais; Data curation Investigation, Methodology and Writing – original draft: B. Chícharo; Data curation, Investigation and Writing – original draft (on specific parts): M. Cuesta, G. Trapasso, R. Porcar, N. Martín, R. Villa, P. Lozano.

Declaration of competing interests

No competing interests

Acknowledgements

This work was supported by the DoE 2023–2027 (MUR, AIS. DIP.ECCELLENZA2023_27.FF project). N. M. acknowledge the “Ramon y Cajal” contract with code RYC2021-033167-I funded MCIN/AEI/10.13039/501100011033 and by “ESF investing in your future”, “European Union NextGenerationEU/PRTR”. This work has been partially supported by MICINN-FEDER-AEI 10.13039/501100011033 (PID2021-124695OB-C21, PID2021-124695OB-C22, PID2022-142897OA-I00), MCIN/AEI/10.13039/501100011033, and by project PROMETEO 2024 of ‘‘Conselleria de Educación, Universidades y Empleo’’ (GVA - PROMETEO - CIPROM/2023/57) and European Social Fund. B.C., S.F. and F.A. are grateful to Grand Reims, Département de la Marne et Grand Est for their financial support.

Appendix A. Supplementary data

Supplementary data to this article can be found online.

Bibliography

Annatelli, M., Sánchez-Velandia, J.E., Mazzi, G., Pandeirada, S.V., Giannakoudakis, D., Rautiainen, S., Esposito, A., Thiyagarajan, S., Richel, A., Triantafyllidis, K.S., Robert, T., Guigo, N., Sousa, A.F., García-Verdugo, E., Aricò, F., 2024. Beyond 2,5-furandicarboxylic acid: status quo , environmental assessment, and blind spots of furanic monomers for bio-based polymers. Green Chem. 26, 8894–8941.

Bielski, R., Grynkiewicz, G., 2021. Furan platform chemicals beyond fuels and plastics. Green Chem. 23, 7458–7487.

Biermann, U., Friedt, W., Lang, S., Lühs, W., Machmüller, G., Metzger, J.O., Rüsch Gen. Klaas, M., Schäfer, H.J., Schneider, M.P., 2000. New Syntheses with Oils and Fats as Renewable Raw Materials for the Chemical Industry. Angew. Chem. Int. Ed. 39, 2206–2224.

Burguete, M. I., García-Verdugo, E., Luis, S. V., Restrepo, J. A., 2011. Preparation of polymer-supported gold nanoparticles based on resins containing ionic liquid-like fragments: easy control of size and stability. Phys. Chem. Chem. Phys.13, 14831.

Cho, J.K., Lee, J.-S., Jeong, J., Kim, Bora, Kim, Baekjin, Kim, S., Shin, S., Kim, H.-J., Lee, S.-H., 2013. Synthesis of carbohydrate biomass-based furanic compounds bearing epoxide end group(s) and evaluation of their feasibility as adhesives. J. Adhes. Sci. Technol. 27, 2127–2138.

Dai, J., Peng, Y., Teng, N., Liu, Y., Liu, C., Shen, X., Mahmud, S., Zhu, J., Liu, X., 2018. High-Performing and Fire-Resistant Biobased Epoxy Resin from Renewable Sources. ACS Sustain. Chem. Eng. 6, 7589–7599.

Deng, J., Liu, X., Li, C., Jiang, Y., Zhu, J., 2015. Synthesis and properties of a bio-based epoxy resin from 2,5-furandicarboxylic acid (FDCA). RSC Adv. 5, 15930–15939.

Giulivo, M., Lopez De Alda, M., Capri, E., Barceló, D., 2016. Human exposure to endocrine disrupting compounds: Their role in reproductive systems, metabolic syndrome and breast cancer. A review. Environ. Res. 151, 251–264.

Guadagno, L., Raimondo, M., Vittoria, V., Vertuccio, L., Naddeo, C., Russo, S., De Vivo, B., Lamberti, P., Spinelli, G., Tucci, V., 2014. Development of epoxy mixtures for application in aeronautics and aerospace. RSC Adv 4, 15474–15488.

Hatano, M., Tabata, Y., Yoshida, Y., Toh, K., Yamashita, K., Ogura, Y., Ishihara, K., 2018. Metal-free transesterification catalyzed by tetramethylammonium methyl carbonate. Green Chem. 20, 1193–1198.

Ho, T.-H., Wang, C.-S., 1996. Modification of epoxy resins with polysiloxane thermoplastic polyurethane for electronic encapsulation: 1. Polymer 37, 2733–2742.

Hsieh, A.Y., Haines, R.S., Harper, J.B., 2023. The effects of ionic liquids on the ethanolysis of a chloroacenaphthene. Evaluation of the effectiveness of nucleofugality data to predict reaction outcome. RSC Adv. 13, 21036–21043.

Jin, F.-L., Li, X., Park, S.-J., 2015. Synthesis and application of epoxy resins: A review. J. Ind. Eng. Chem. 29, 1–11.

Liu, Y., Zhao, J., Peng, Y., Luo, J., Cao, L., Liu, X., 2020. Comparative Study on the Properties of Epoxy Derived from Aromatic and Heteroaromatic Compounds: The Role of Hydrogen Bonding. Ind. Eng. Chem. Res. 59, 1914–1924.

Lozano, P, García-Verdugo, E., Bernal, J. M., Izquierdo, D. F., Burguete, M. I., Sánchez-Gómez, G., Luis, S. V., 2012. Immobilised Lipase on Structured Supports Containing Covalently Attached Ionic Liquids for the Continuous Synthesis of Biodiesel in scCO2. ChemSusChem 2012, 5, 790.

Lozano, P., Bernal, J.M., Nieto, S., Gomez, C., Garcia-Verdugo, E., Luis, S.V., 2015. Active biopolymers in green non-conventional media: a sustainable tool for developing clean chemical processes. Chem. Commun. 51, 17361–17374.

Lozano, P., García‐Verdugo, E., Bernal, J.M., Izquierdo, D.F., Burguete, M.I., Sánchez‐Gómez, G., Luis, S.V., 2012. Immobilised Lipase on Structured Supports Containing Covalently Attached Ionic Liquids for the Continuous Synthesis of Biodiesel in scCO2. ChemSusChem 5, 790–798.

Marotta, A., Ambrogi, V., Cerruti, P., Mija, A., 2018. Green approaches in the synthesis of furan-based diepoxy monomers. RSC Adv. 8, 16330–16335.

Meier, M.A.R., Metzger, J.O., Schubert, U.S., 2007. Plant oil renewable resources as green alternatives in polymer science. Chem. Soc. Rev. 36, 1788.

Meng, J., Zeng, Y., Chen, P., Zhang, J., Yao, C., Fang, Z., Guo, K., 2019a. New ultrastiff bio-furan epoxy networks with high Tg: Facile synthesis to excellent properties. Eur. Polym. J. 121, 109292.

Meng, J., Zeng, Y., Zhu, G., Zhang, J., Chen, P., Yao, C., Fang, Z., Guo, K., 2019b. Sustainable Bio-based Furan Epoxy Resin with Flame Retardancy. Polym. Chem. 7, 36–43.

Migowski, P., Lozano, P., Dupont, J., 2023. Imidazolium based ionic liquid-phase green catalytic reactions. Green Chem. 25, 1237–1260.

Nameer, S., Larsen, D.B., Duus, J.Ø., Daugaard, A.E., Johansson, M., 2018. Biobased Cationically Polymerizable Epoxy Thermosets from Furan and Fatty Acid Derivatives. ACS Sustain. Chem. Eng. 6, 9442–9450.

Negrell, C., Cornille, A., De Andrade Nascimento, P., Robin, J., Caillol, S., 2017. New bio‐based epoxy materials and foams from microalgal oil. Eur. J. Lipid Sci. Technol. 119, 1600214.

Ng, F., Couture, G., Philippe, C., Boutevin, B., Caillol, S., 2017. Bio-Based Aromatic Epoxy Monomers for Thermoset Materials. Molecules 22, 149.

Peris, E, Porcar, R, Burguete, M. I., García-Verdugo, E., Luis, S. V., 2019. Supported Ionic Liquid-Like Phases (SILLPs) as Immobilised Catalysts for the Multistep and Multicatalytic Continuous Flow Synthesis of Chiral Cyanohydrins. ChemCatChem 11, 1955.

Rahman, Md.M., Akhtarul Islam, M., 2022. Application of epoxy resins in building materials: progress and prospects. Polym. Bull. 79, 1949–1975.

Rong, L., Su, J., Li, Z., Liu, X., Zhang, D., Zhu, J., Li, X., Zhao, Y., Mi, C., Kong, X., Wang, G., 2024. Silicon Hybridization for the Preparation of Room-Temperature Curing and High-Temperature-Resistant Epoxy Resin. Polymers 16, 634.

Sandler, S.R., Berg, F.R., 1966. Room temperature polymerization of glycidol. J. Polym. Sci. 4, 1253–1259.

Schindl, A., Hawker, R.R., Schaffarczyk McHale, K.S., Liu, K.T.-C., Morris, D.C., Hsieh, A.Y., Gilbert, A., Prescott, S.W., Haines, R.S., Croft, A.K., Harper, J.B., Jäger, C.M., 2020. Controlling the outcome of SN 2 reactions in ionic liquids: from rational data set design to predictive linear regression models. Phys. Chem. Chem. Phys. 22, 23009–23018.

Sherrington, D.C., 1998. Preparation, structure and morphology of polymer supports. Chem. Commun. 2275–2286.

Sprenger, S., 2013. Epoxy Resin Composites with Surface‐modified Silicon Dioxide Nanoparticles: A Review. J. of Appl. Polym. Sci. 130, 1421–1428.

Tanaka, S., Nakajima, Y., Ogawa, A., Kuragano, T., Kon, Y., Tamura, M., Sato, K., Copéret, C., 2022. DNP NMR spectroscopy enabled direct characterization of polystyrene-supported catalyst species for synthesis of glycidyl esters by transesterification. Chem. Sci. 13, 4490–4497.

Tanaka, S., Nakashima, T., Satou, N., Oono, H., Kon, Y., Tamura, M., Sato, K., 2019. Epoxide as precatalyst for metal-free catalytic transesterification. Tetrahedron Lett. 60, 2009–2013.

Trapasso, G., Annatelli, M., Dalla Torre, D., Aricò, F., 2022. Synthesis of 2,5-furandicarboxylic acid dimethyl ester from galactaric acid via dimethyl carbonate chemistry. Green Chem. 24, 2766–2771.

Trapasso, G., Chícharo, B., Gherardi, T., Redolfi-Bristol, D., Aricò, F., 2023. Iron(III) Sulfate-Mediated Synthesis of 2,5-Furandicarboxylic Acid Dimethyl Ester from Galactaric Acid. Catalysts 13, 1114.

Trzebicka, B., Watach, W., Kurcok, P., Kowalczuk, M., 2024. Ring-opening (co)polymerization strategies of selected oxacyclic monomers to control and provide tailored polymers with desired properties. Polym Adv Technol. 35.

Verma, C., Olasunkanmi, L.O., Akpan, E.D., Quraishi, M.A., Dagdag, O., El Gouri, M., Sherif, E.-S.M., Ebenso, E.E., 2020. Epoxy resins as anticorrosive polymeric materials: A review. React. Funct. Polym. 156, 104741.

Villa, R., Alvarez, E., Porcar, R., Garcia-Verdugo, E., Luis, S.V., Lozano, P., 2019. Ionic liquids as an enabling tool to integrate reaction and separation processes. Green Chem. 21, 6527–6544.

Villa, R., Porcar, R., Nieto, S., Donaire, A., Garcia-Verdugo, E., Luis, S.V., Lozano, P., 2021. Sustainable chemo-enzymatic synthesis of glycerol carbonate (meth)acrylate from glycidol and carbon dioxide enabled by ionic liquid technologies. Green Chem. 23, 4191–4200.

Voirin, C., Caillol, S., Sadavarte, N.V., Tawade, B.V., Boutevin, B., Wadgaonkar, P.P., 2014. Functionalization of cardanol: towards biobased polymers and additives. Polym Chem 5, 3142–3162.

Weber, C.C., Masters, A.F., Maschmeyer, T., 2013. Structural features of ionic liquids: consequences for material preparation and organic reactivity. Green Chem. 15, 2655.

Yang, H., Shafaghat, H., Öman, T., Johansson, A.-C., 2025. Sustainable production of bio-based epoxy resins using the phenolics produced via atmospheric ex-situ catalytic hydropyrolysis of biomass. J. Ind. Eng. Chem. S1226086X25000012.

Zhang, C., Xue, J., Yang, X., Ke, Y., Ou, R., Wang, Y., Madbouly, S.A., Wang, Q., 2022. From plant phenols to novel bio-based polymers. Prog. Polym. Sci. 125, 101473.

Zhang, D., Dumont, M., 2017. Advances in polymer precursors and bio‐based polymers synthesized from 5‐hydroxymethylfurfural. J. Polym. Sci. Part Polym. Chem. 55, 1478–1492.

Zhu, Y., Romain, C., Williams, C.K., 2016. Sustainable polymers from renewable resources. Nature 540, 354–362.